Cable TIES

| Material : | Polyamide 6.6 |
| --- | --- |
| Wide: | 2.5mm |
| Long: | 200mm |
| Flammability Of Raw Material : | UL 94 - V2 |
| Humidity Absorption : | 2,7%-2,8% (23°C -50% R.H.) |
| Installation Temperature : | -10°C ~+85°C |
| Working Temperature : | -40°C ~+85°C |
| Max Sustaiaable Tempeature For Short Time:Certificate: | +110°C |
| Features： | Releasable cable ties are available in two different designs. One design has an extended pawl or locking mechanism in the head of the tie which can be released with a thumbnail force. The second design has a large horizontal tab feature which releases the tie with a push onto the tab. |
|  | Good resistance to bases, oils, greases, oil derivates,chloride solvents. Limited resistance to acids. Not resistant to phenols. Carbon black addiction gives a better UV resistance (only for Black Cabe Ties) |
| Application: | Used to bundle cables, wires, conducts, plants or other things in the industry of electrical & electronic, lighting, hardware, pharmaceutical, chemical, computer, machinery, agriculture, etc. |

Part number: CABLE-T-200B

Barcode: 8400800029935